Appendix A: Supplementary Information

The unified theoretical model for Triboelectric Nanogenerators

R.D.I.G. Dharmasenaa, K.D.G.I. Jayawardenaa, C.A. Millsa,b, R.A. Doreyc, S.R.P. Silvaa*

a Advanced Technology Institute, Department of Electrical and Electronic Engineering, University of Surrey, Guildford, Surrey, GU2 7XH, United Kingdom. Email: s.silva@surrey.ac.uk

b Advanced Coatings Group, Tata Steel Research Development and Technology, Voyager Building 9, Sir William Lyon Road, Coventry CV4 7EZ, United Kingdom.

c Centre for Engineering Materials, Mechanical Engineering Sciences, University of Surrey, Guildford, Surrey, GU2 7XH, United Kingdom.

Contents:

Supplementary Notes 1 - 6

Supplementary Figures S.1 – S.9

Supplementary Tables S.1 – S.4

Fig. S1: Graphical representation of a metal-dielectric VCSTENG.

Fig. S1: Graphical representation of a metal-dielectric VCSTENG.

Supplementary Note 1: Metal-dielectric VCSTENG

The TENG layers are triboelectrically charged during contact-separation of the device (Fig. S1). σT on the dielectric layer is assumed to saturate and remain unchanged after several initial contacts, with equal amounts of charges of opposite polarity transferred to the metal sheet surface.[1–3] The accumulation of output charges on the metal sheet is assumed to take place on the metal-free space interface. When the TENG layers are moved relative to each other, there will be a charge transfer between the electrodes as they attempt to reach an equipotential status due to the distance-dependent nature of the electric fields.[1]

The electric field originating from the metal sheet is influenced by the initial charge due to triboelectric charging and the charge transfer between the electrodes during TENG layer movement. For the dielectric sheet, the triboelectric charges are generally considered to be statically fixed to the contact surface[1], and they can be clearly identified as different from the induced output charges appearing on the attached electrode. Moreover, triboelectric charges are not static on the metal sheet as they get involved in the charge transfer between the electrodes, and the electric field originating from the metal sheet is due to the remaining charges on the metal sheet at a given separation of TENG layers. However, it is convenient to represent this residual charge as a balance between the output charge and the initial triboelectric charge considering they have opposite polarities (Fig. S1).

Using eqn (2) and (3) the potential of the metal sheet (Φ1) and attached electrode (Φ2) can be given as,

Φ1=-σuπε00zt+x1fxdx+σTπε00ztfxdx 						(S1)

Φ2=σuπε10zt+x1fxdx-σTπε1x1zt+x1fxdx 					(S2)

where x1 and ε1 are the thickness and dielectric constant of the dielectric sheet. In the short circuit configuration, using eqn (5),

σu=σT(1ε1x1zt+x1fxdx+1ε00z(t)fxdx)(1ε0+1ε1)0zt+x1fxdx 							(S3)

Using eqn (6), the current through a load R can be evaluated using,

LWRdσudt+σuπ(1ε0+1ε1)0zt+x1fxdx-σTπ1ε1x1zt+x1fxdx+1ε00ztfxdx=0 	(S4)

Fig. S2: Graphical representation of a SETENG, with (a) a non-parallel secondary electrode arrangement, and (b) a grounded primary electrode through an output load. The TENG layers correspond to the colour code description shown in Fig. S1.

Fig. S2: Graphical representation of a SETENG, with (a) a non-parallel secondary electrode arrangement, and (b) a grounded primary electrode through an output load. The TENG layers correspond to the colour code description shown in Fig. S1.

Supplementary Note 2: SETENG configurations

A non-parallel secondary electrode SETENG is shown in Fig. S2a. In this demonstration, a similar material is used for both the electrodes. The potential of the primary electrode depends on the electric field originated from the dielectric sheet, and the amount of charges appearing on itself due triboelectric charging and the charge transfer with the secondary electrode. The potential of the secondary electrode depends solely on the charges obtained due to the charge exchange with the primary electrode. The movement of the triboelectrically charged dielectric sheet relative to the primary electrode causes the potential of the primary electrode to change due to the distance-dependent electric field behaviour, causing a charge transfer between the electrodes to nullify their potential difference. Hence, applying the respective electric field components to eqn (2) and (3), the DDEF equations can be developed for the non-parallel secondary electrode SETENG (section 3.5).

Instead of using a secondary electrode, primary electrode can be connected to the ground via a load (Fig. S2b). The charge transfer then occurs between the ground and the primary electrode through the load resistor, such that the potential of the electrode is made equal to the ground potential (zero). Considering the potential (Φ1) of the electrode and using eqn (2),

Φ1=-σuπε00∞fxdx+σTπε00ztfxdx 							(S5)

Furthermore, Φ2=0 (ground potential). For the short circuit condition, using eqn (5),

σu=σT0ztfxdx0∞fxdx 										(S6)

The current flow through the external load can be estimated using eqn (6),

LWRdσudt+σuπε00∞fxdx-σTπε00z(t)fxdx=0 						(S7)

Supplementary Note 3: Experimental procedures

Fig. S3: (a) The bespoke test setup for the characterization of vertical charge polarization TENGs. The modification of the setup for the (b) Non-parallel secondary electrode SETENG, and, (c) Dielectric free-standing layer FSTENG.

Fig. S3: (a) The bespoke test setup for the characterization of vertical charge polarization TENGs. The modification of the setup for the (b) Non-parallel secondary electrode SETENG, and, (c) Dielectric free-standing layer FSTENG.

Testing apparatus

The contact-separation movement of the TENG layers was controlled using the motion control setup shown in Fig. S3. In the typical configuration for VCSTENG (Fig. S3a) and SETENG (Fig. S3b) testing, the voice coil linear actuator was connected to a guided moving stage, and a metal holder carrying one of the TENG layers was attached to it. The metal holder was electrically isolated from the rest of the apparatus by an insulating sheet. The electrical output was obtained using a connecter attached to the metal holder.

A load cell carrying a similar metal holder was fixed in front of the stage such that the holder is aligned and in parallel to the movable TENG layer. The force applied during the contact of triboelectric surfaces was controlled to be approximately 20 N for all the TENG types, similar to the test procedure followed in our previous work[1].  For the VCSTENG, an insulating layer was again used to electrically isolate the second metal holder (which carries the second TENG layer) from the rest of the apparatus framework, and the output was obtained through the connectors. For the SETENG on the other hand, the secondary electrode was kept non-parallel, away from the primary electrode (Fig. S3b).

The moving stage of the apparatus was modified to accommodate an additional parallel plate for the FSTENG (Fig. S3c). The steel electrodes were attached on the inner sides of these plates with a separation (g) of 8.2 mm between them, and the PMMA layer was placed parallelly between the metal electrodes using additional clamps connected to the optical table. During the testing process, the motion of the moving stage resulted in steel electrodes moving with respect to the PMMA layer, providing the required relative movement for the FSTENG layers.

The respective triboelectric surfaces of each TENG type were pre-charged to ensure the surfaces were saturated with triboelectric charges prior to testing, as described in our previous work[1]. For the pre-charging of the FSTENG, the two steel electrodes were uniformly contacted against the corresponding sides of the PMMA sheet.

Characterization methods

Voltage measurements were obtained by separating the pre-charged TENG layers to different separations from contact, while charge, current, and power measurements were obtained by using sinusoidal contact-separation movements of the TENG layers. The peak increment in voltage, charge and current from the recorded readings were selected for the analysis.

During the testing of the FSTENG, the contact position of the PMMA layer with the front steel layer (towards the load cell side of Fig. S3) was selected as the reference contact position (RCP). The measurement of voltage and output charge was done with respect to the output values at the RCP point (considering the output at the RCP as zero).

Fig. S4: Comparison of the experimental outputs for the PDMS-stainless steel VCSTENG and the corresponding simulated outputs. (a) The overall error between the DDEF model predictions and experimental outputs at different σT considering Isc and Qsc. (b) Comparison between the DDEF model simulations and experimental outputs for Qsc against increasing H (n=1 Hz). (c) The overall error between the experimental Isc and Qsc and the predictions from the previously accepted model[4], at different σT. (d) Comparison between the experimental outputs and the predictions from the DDEF model and previously accepted model[4], for Isc against increasing H (n=1 Hz). (e) Maximum output power for Ag – PTFE TENG reported previously (indicated as previous study 2 - ref [46]) compared with corresponding DDEF predictions. Error bars indicate the standard deviation of 10 readings.

Fig. S4: Comparison of the experimental outputs for the PDMS-stainless steel VCSTENG and the corresponding simulated outputs. (a) The overall error between the DDEF model predictions and experimental outputs at different σT considering Isc and Qsc. (b) Comparison between the DDEF model simulations and experimental outputs for Qsc against increasing H (n=1 Hz). (c) The overall error between the experimental Isc and Qsc and the predictions from the previously accepted model[4], at different σT. (d) Comparison between the experimental outputs and the predictions from the DDEF model and previously accepted model[4], for Isc against increasing H (n=1 Hz). (e) Maximum output power for Ag – PTFE TENG reported previously (indicated as previous study 2 - ref [46]) compared with corresponding DDEF predictions. Error bars indicate the standard deviation of 10 readings.

Supplementary Note 4: The dielectric-metal VCSTENG

Table S1: Parameters of the PDMS-stainless steel VCSTENG.

| Length (L) | 5 cm |
| --- | --- |
| Width (W) | 5 cm |
| Dielectric constant of the dielectric contact layer (ε1) | 3.24 |
| Thickness of the dielectric contact layer | 220 µm |
| Triboelectric charge density (σT) | 30 µC/m2 |

The experimental and simulated outputs (for Isc and Qsc) were compared to obtain the σT with the minimum error (Fig. S5a for the DDEF model and Fig. S5c for the previously accepted model[4]), and used as the triboelectric charge density in respective simulations. The difference between the experimental and simulated value was obtained as a fraction of the experimental output, and the modulus of this fraction was calculated. The sum of this error fraction for the short circuit outputs were calculated (accumulated error fraction) and graphed against σT to determine the minimum error (Fig. S5a, c). The charge density corresponding to the minimum error was then used as the approximated σT for the stainless steel – PDMS triboelectric surfaces. The DDEF model provided the minimum error at σT=30 µC/m2 whereas the previously accepted model[4] indicated σT=20 µC/m2 as the charge density with the minimum error.

As depicted in Fig. S4b, there is some mismatch between the experimental and theoretical charge outputs, which seems more prominent at larger separations. This variation can be understood considering that the estimation of σT=30 µC/m2 is intended to match both Isc and Qsc outputs at different H and n values, and the current and charge measurements were conducted using two different measurement units using two separate tests (Kiethley 6487 picoammeter for current, Keithley 6517B electrometer for charge).

Table S2: Device parameters for previously reported metal-dielectric VCSTENGs.

| Parameter | Previous Study 1 (ref [45] of main text) | Previous Study 2 (ref [46] of main text) |
| --- | --- | --- |
| Thickness of the dielectric layer | 90 µm | 200 µm |
| Area of the TENG layers | 49 cm2 | 8.75 cm2 |
| Relative permittivity of the dielectric | 2.3 | 2.1 |
| Maximum separation | 5 mm | 1.5 mm |
| Frequency (n) | 1 Hz | 3 Hz |
| σT | 17.5 µC/m2 | 90 µC/m2 (approximated) |
| Load resistance (R) | 0 Ω (short circuit) | 500 MΩ |

Supplementary Note 5: Output comparison for SETENG

Fig. S5: (a)-(c) Comparison of the experimental outputs with the predictions from the DDEF model, for the non-parallel secondary electrode SETENG; (a) DDEF model predictions, and (b) experimental outputs for peak  Qsc at increasing H (n=1 Hz). (c) Comparison of experimental Voc with the predictions from the DDEF model. (d)-(e) Comparison of the previously published results with the corresponding simulations from the DDEF model; (d) output charge, and (e) Voc against increasing H for the parallel secondary electrode SETENG in study 4 (ref [20] of the main text). Error bars indicate the standard deviation of 10 readings. For (a), the solid markers indicate the simulated points and the line indicates the interpolated trend.

Fig. S5: (a)-(c) Comparison of the experimental outputs with the predictions from the DDEF model, for the non-parallel secondary electrode SETENG; (a) DDEF model predictions, and (b) experimental outputs for peak  Qsc at increasing H (n=1 Hz). (c) Comparison of experimental Voc with the predictions from the DDEF model. (d)-(e) Comparison of the previously published results with the corresponding simulations from the DDEF model; (d) output charge, and (e) Voc against increasing H for the parallel secondary electrode SETENG in study 4 (ref [20] of the main text). Error bars indicate the standard deviation of 10 readings. For (a), the solid markers indicate the simulated points and the line indicates the interpolated trend.

Table S3: Device parameters for SETENGs reported in previously studies.

| Parameter | Previous Study 3 (ref [47] of the main text) | Previous Study 4 (ref [21] of the main text) |
| --- | --- | --- |
| Area of the TENG layers | 100 cm2 | 25 mm2 |
| Gap distance between the electrodes | 2 cm | 1 mm |
| σT | 10 µC/m2 | 8 µC/m2 |
| Separation velocity | 1 m/s | 1 m/s |

Fig. S6: Comparison of  Voc for the VCSTENG and SETENG at different triboelectric layer separations: (a) predictions from the DDEF model, and, (b) experimental results. Error bars indicate the standard deviation of 10 readings.

Fig. S6: Comparison of  Voc for the VCSTENG and SETENG at different triboelectric layer separations: (a) predictions from the DDEF model, and, (b) experimental results. Error bars indicate the standard deviation of 10 readings.

Performance of a SETENG relative to a VCSTENG

For both VCSTENG and SETENG, the negative and positive triboelectric charges rest on the same plane when z(t)=0, resulting in no net output. Considering the VCSTENG (Fig. S1), the overall electric field will be negative at the dielectric-attached electrode interface as z(t) is increased, resulting in a negative potential of the attached electrode. Similarly, the potential of the metal sheet will be positive. When the electrodes are connected, a charge transfer takes place between the electrodes to equilibrate the potential difference, and the output charge density reaches σT at sufficiently large z(t) (for a reasonably small dielectric thickness)[1].

Considering the SETENG (Fig. 1a), potential of the primary electrode becomes positive when z(t) is increased. The potential of the secondary electrode also becomes positive with a lower magnitude than that of Node 2 (due to distance-dependent electric fields), considering the relative positioning of the TENG layers. Therefore, the potential difference between the electrodes is lower for the SETENG than for a corresponding VCSTENG. When the electrodes are connected, a charge transfer take place between them, where the output charge density reaches close to σT/2 at sufficiently large z(t) (Fig. S7), which is again lower than the VCSTENG. The low charge transfer combined with the low potential difference for a given separation results in the lower current and power output for a SETENG, relative to a comparable VCSTENG (Fig. 4, Fig. S6).

Fig. S7: The output predictions using the DDEF model for a parallel secondary electrode SETENG, at different d. (a) short circuit output charge density against increasing H, and (b) Voc against increasing TENG layer separations.

Fig. S7: The output predictions using the DDEF model for a parallel secondary electrode SETENG, at different d. (a) short circuit output charge density against increasing H, and (b) Voc against increasing TENG layer separations.

Theoretical prediction of the influence of electrode separation (d) on SETENG output

The device parameters used for simulations in Fig. S7 are identical to that for a non-parallel secondary electrode TENG (section 4.2), with the exception being the secondary electrode placed in parallel (similar to Fig. 1a). σT=30 µC/m2 was used for the DDEF model simulations.

As per DDEF predictions σT saturates around 14.8 µC/m2 at increasing H, when d is relatively small (<1 mm), reaching a value close to σT/2. The output charge decreases as d is increased (Fig. S7a), agreeing with the trends suggested by the previously accepted model for SETENGs[2]. However, the DDEF model predicts that the output charge trend would become fixed at larger d (>10 cm), saturating around 13.9 µC/m2. This is contradictory to the previously accepted model[2], which predicts the output charge to reach zero when d is significantly large.

When d is increased, the electric field interactions of the primary electrode and the dielectric layer, against the secondary electrode becomes weak due to the distance-dependent nature of the electric fields. Hence, the potential of secondary electrode depends only on the remaining output charges on itself resulting from the charge transfer with the primary electrode. This is equivalent to the case of a non-parallel secondary electrode SETENG (section 3.5). Incidentally, the charge output for a parallel-secondary electrode SETENG show an identical behaviour to the corresponding non-parallel secondary electrode SETENG (Fig. S7a) at large d values. Furthermore, the DDEF simulations suggest a significant increase of Voc when d is increased (Fig. S7b), which saturates at large d values, agreeing with the previously predicted trends[2]. At sufficiently large d values, the Voc behaviour becomes identical to the non-parallel secondary electrode scenario (Fig. S7b).

Supplementary Note 6: FSTENG output comparison

Fig. S8: (a) Overall error between the simulated and experimental results for the stainless steel and PMMA triboelectric surfaces, considering the short circuit outputs of the control VCSTENG, and (b) the corresponding Qsc fit at σT=2 µC/m2. (c) Comparison of Voc predictions from the DDEF model and the experimental outputs, for the FSTENG. Error bars indicate the standard deviation of 10 readings.

Fig. S8: (a) Overall error between the simulated and experimental results for the stainless steel and PMMA triboelectric surfaces, considering the short circuit outputs of the control VCSTENG, and (b) the corresponding Qsc fit at σT=2 µC/m2. (c) Comparison of Voc predictions from the DDEF model and the experimental outputs, for the FSTENG. Error bars indicate the standard deviation of 10 readings.

Table S4: Parameters of the FSTENG reported in previous study 5 (ref [22] of the main text).

| Area of the TENG layers | 16 inch2 |
| --- | --- |
| Gap distance between the electrodes | 7 mm |
| Total thickness of free standing layer | 4.175 mm |
| Overall relative permittivity of the free-standing layer | 2.53 |
| σT | 2 µC/m2 (Approximated) |

Performance of a FSTENG relative to a VCSTENG

Considering the FSTENG (Fig. 1d), the potential of the electrodes is balanced when the dielectric sheet is in the mid position between the metal sheets (zt=(g-k)/2). When zt decreases, the potential of the Node 1 relative to Node 4 becomes negative, as Nodes 2 and 3 with negative triboelectric charges are moving closer to Node 1, and away from Node 4. When zt=0, an output charge density corresponding to approximately σT is transferred to Node 1 and the charge density on the Node 4 corresponds to approximately -σT (for reasonably small k). In contrary, when zt is increased such that Node 3 and Node 4 are in contact, the charge density on Node 1 will reduce and correspond to -σT and the value on Node 4 will be σT. Hence, with respect to z(t)=0 position (RCP position), an output charge corresponding to 2σT is exchanged between the electrodes at maximum z(t) (Fig. 6 a, d), as opposed to a VCSTENG where the maximum output charge density is limited to σT (Supplementary Note 6).  The charge output of the VCSTENG tends to increase and saturate more rapidly relative to a FSTENG, and as a result the peak output current of the VCSTENG is higher (Fig. 6 b, e). This results in the higher power output of the VCSTENG, in most of the resistances used in the experiments and simulations (Fig. 6c, f).

Fig. S9: Comparison of the DDEF predictions for FSTENG against different g. The short circuit (a) peak output charge density, and (b) peak current density, against increasing H (n=1 Hz), for different g values.

Fig. S9: Comparison of the DDEF predictions for FSTENG against different g. The short circuit (a) peak output charge density, and (b) peak current density, against increasing H (n=1 Hz), for different g values.

Theoretical prediction of the influence of electrode separation (g) on FSTENG outputs

The output predictions for a FSTENG at different electrode separations (g) is depicted in Fig. S9. The identical device parameters used for the FSTENG (section 4.3) is used for this simulation at changing g (Fig. S9). The peak short circuit output charge density increases linearly when g is relatively low, and deviates from the linear behaviour when g is significantly increased (Fig. S9a). The maximum charge density reaches close to 3.9 µC/m2 (approximately 2σT) for all simulated g values when H is maximized. The short circuit current density shows a similar behaviour, where the outputs show a linear trend at relatively low g values, and deviates from the linear behaviour at higher g values (Fig. S9b).

The linear output behaviour of the FSTENG can be explained using the DDEF model. Considering the FSTENG (Fig. 1d), when z(t) is increased starting from zt=0 , the influence of the electric fields originating from free-standing layer (Nodes 2 and 3), on Node 1 decrease rapidly and become significantly low at sufficiently large z(t). This causes the potential of Node 1 to be more positive, at a decreasing rate. At the same time, the distance between free-standing layer and Node 4 reduces, creating a rapid rise on the influence of its electric fields on Node 4. This increasing electric field interaction makes the positive potential of Node 4 to decease at an increasing rate, hence relative to Node 4, Node 1 becomes more positive. Therefore, the drop in the rate of the potential increment of Node 1 due to increasing z(t) is compensated by the rise in the rate of potential decrement of Node 4, resulting in the overall linear response of the voltage, and accordingly the current and charge, for relatively small g (Fig. S9). Considering g is significantly large with respect to TENG layer dimensions, when z(t) is increased from zt=0, the increase in the potential of Node 1 takes place at a decreasing rate similar to the previous case. However, as a consequence of the increased decay of the electric fields due to higher separation with Node 4, the free-standing layer is not capable of influencing an equivalent rapid change in the potential of Node 4. Hence, the output behaviour of the FSTENG deviates from its characteristic linear trend at relatively large g values (Fig. S9).

Supplementary References

[1]	R.D.I.G. Dharmasena, K.D.G.I. Jayawardena, C.A. Mills, J.H.B. Deane, J. V. Anguita, R.A. Dorey, S.R.P. Silva, Triboelectric nanogenerators: providing a fundamental framework, Energy Environ. Sci. 10 (2017) 1801–1811. doi:10.1039/C7EE01139C.

[2]	S. Niu, Y. Liu, S. Wang, L. Lin, Y.S. Zhou, Y. Hu, Z.L. Wang, Theoretical Investigation and Structural Optimization of Single-Electrode Triboelectric Nanogenerators, Adv. Funct. Mater. 24 (2014) 3332–3340. doi:10.1002/adfm.201303799.

[3]	S. Niu, Y. Liu, X. Chen, S. Wang, Y.S. Zhou, L. Lin, Y. Xie, Z.L. Wang, Theory of freestanding triboelectric-layer-based nanogenerators, Nano Energy. 12 (2015) 760–774. doi:10.1016/j.nanoen.2015.01.013.

[4]	S. Niu, S. Wang, L. Lin, Y. Liu, Y.S. Zhou, Y. Hu, Z.L. Wang, Theoretical study of contact-mode triboelectric nanogenerators as an effective power source, Energy Environ. Sci. 6 (2013) 3576. doi:10.1039/c3ee42571a.